## Slide 1: Maraging Steel Blades: Manufacturing Process Flowchart
Thin suspension blades: ground, machined, rolled (2.2)
Material: Maraging C-250 or C-300, with blades aligned with grain (2.1)
Dimensional check (2.3), Cleanliness (2.4)
Bake to prevent hydrogen embrittlement (2.6). If the bake to drive off phosphorus (next step) can be done within 1 hour of plating this bake can be missed out.
Age hardening bake (2.7.1)
Default Process for Thin Blades
Alternative Process for Thin Blades ( ref section 3)
Dimensional check (2.8)
Age hardening bake (2.7.1)
Electropolishing/electrocleaning, Nickel plating (2.5)
Bake to prevent hydrogen embrittlement (2.6). If the age hardening step (next step) can be done within 1 hour of plating this bake can be missed out.
Bake to drive off phosphorous (3)
Dimensional check (2.8)
Thick seismic isolation blades: two options.
For flat shape: machined
For curved shape: EDM oversize (2.2)
Age hardening bake (2.7.2)
For flat shape: ground to finished size
For curved shape EDM to finished size
Electropolishing/electrocleaning, Nickel plating (2.5)
Electropolishing/electrocleaning, Nickel plating (2.5)
Bake to prevent hydrogen embrittlement (2.6). If the bake to drive off phosphorus (next step) can be done within 1 hour of plating this bake can be missed out.
Bake to drive off phosphorous (3)
Dimensional check (2.8)
Default Process for Thick Blades
Dimensional check (2.3), Cleanliness (2.4)