| APPROVALS | DATE | REV | DCN NO. | BY | CHECK | DCC | DATE |
| --- | --- | --- | --- | --- | --- | --- | --- |
| AUTHOR: V. Parames | 01/23/08 | A | E080042-A |  |  |  |  |
| CHECKED: G Billingsley | 04/04/08 | A |  |  |  |  |  |
| APPROVED: |  |  |  |  |  |  |  |
| DCC RELEASE |  |  |  |  |  |  |  |

This document specifies the material to be used for PR3 and SR3.

Applicable Documents

LIGO-D080053-A 		AdLIGO R3 Blank

MIL-G-174-B 			Glass, Optical

Requirements

Physical Dimensions 			per LIGO- D080053-A AdLIGO R3 Blank

Clear Aperture 				Central 200  mm

Serial Number	Blanks shall be serialized as R3XX, where XX increments starting at 01

Material					Fused silica

Final shaping	Shaping shall be performed using a progression of grit size ending with a 320 or smaller grit tool.

Defect depth 				Maximum on any surface or corner is less than 0.5 mm

Birefringence				< 5 nm/cm

Bubble and Inclusion Cross section 	No bubbles or inclusions within 5mm of the flat surface within the clear aperture

| Specification | Method | Frequency of Inspection | Data Delivered |
| --- | --- | --- | --- |
| Physical Dimensions | Visual Inspection | 100% | Diameter Thickness |
| Serial number | Visual Inspection | 100% | Inspection Report included with Certification |
| Material | Process Control Material Certification | 100% | Inspection Report included with Certification |
| Defect depth | Visual Inspection | 100% | Hand sketch indicating location and dimensions |
| Birefringence | Process Control Material Certification | 100% | Inspection Report included with Certification |
| Inclusions | Visual Inspection | 100% | Hand sketch indicating location and dimensions |

Table 1: MEASUREMENT MATRIX: FREQUENCY AND METHOD