	[image: image1.png]LIGO




	 Laser Interferometer Gravitational Wave Observatory

Specification
	E030245
	-A-
	D

	
	
	Drawing No
	Rev.
	Group

	
	
	Sheet 1
	of
	1

	70 x 60 mm, 15mmCC sapphire Q substrate



	APPROVALS
	DATE
	REV
	DCN NO. 
	BY 
	CHECK 
	DCC
	DATE

	AUTHOR: G. Billingsley
	7-29-03
	A
	E030246-00
	
	
	
	5-5-03

	CHECKED:
	
	
	
	
	
	
	

	APPROVED:
	
	
	
	
	
	
	


Purpose:  These Flat-Concave sapphire substrates are to be used in investigations into sapphire Q and thermal noise.

Applicable Documents:  LIGO-D030385  15mm CC Sapphire Q Substrate

Material:  HEMLITE or Better single crystal sapphire














Orientation:  A axis ± 2 degrees


Diameter:  70.0 mm +/- 0.2 mm














Thickness:  60.0 mm +/- 0.2 mm

Wedge:  30 ± 5 minutes, parallel to the c axis of the material within 3 degrees



Other Mechanical dimensions:  Bevel, cylindricity and runout to best commercial practice

Polish:  All surfaces polished out of gray, including bevel and cylinder

Surface Figure side 1: Central hollow with depth of 5.0 mm +/- 0.2 mm


Offset of central hollow < 0.2mm


Radius of curvature of hollow is 15.84 mm


Side 1 Hollow Figure Precision: ≤ 1  at 633 nm


Side 1 Hollow microroughness: ≤ 1A, "best effort"


Side 1 Annulus figure, nominally flat <  /4, PV at 633 nm


Side 1 Annulus microroughness: Super-polished, ≤ 2 A














Surface Figure side 2:  Nominally flat,  /4, PV at 633 nm


Microroughness side 2:  Super polish < 2 Angstroms RMS






LIGO Form CS-02 (11/00)


[image: image2.png]LIGO



_1025452889.bin

