| Originator | Cognizant Engineer | Ext./Phone# | Project | Account Number |
| --- | --- | --- | --- | --- |
| Stephany Foley | Ken Mason | 617-324-5250 | E-LIGO SEI HAM |  |

| Dwg/Part Number |  | Part Description / Material |  | Qty |
| --- | --- | --- | --- | --- |
| 20007935 D071251 -00 D071251 -01 D071251 -02 D071251 -03 D071251 -04 D071201 D071200 -00 D071200 -01 D071200 -02 D071200 -03 D071200 -04 D071200 -06 D071141 -00 through -10 D071136 -00 D071136 -01 D071003 20007934 (aka D070470) D071103 D071471 |  | locator, spherical pin kinematic lock ligo D047935B, 440C stainless gang barrel nut, 17-4 PH stainless steel (3_8-16 w_2 x 3.0) gang barrel nut, 17-4 PH stainless steel (3_8-16 w_4 x 2.5) gang barrel nut, 17-4 PH stainless steel (1_2-13 w_2 x 3.0) gang barrel nut, 17-4 PH stainless steel (1_2-16 w_3 x 2.5) gang barrel nut, 17-4 PH stainless steel (1_2-16 w_4 x 2.5) mass spacer, 304 SS adjustment masses, 304 SS adjustment masses, 304 SS adjustment masses, 304 SS adjustment masses, 304 SS adjustment masses, 304 SS adjustment masses, 304 SS shim, 304 SS SHCS, custom captive, 18-8 SS SHCS, custom captive, 18-8 SS Support post cap, 304 SS Locker sleeve- stainless with Balinit coating—NOTE: treat as stainless Flexure Mount / stainless Flexure Cups / stainless --where’s 6th one?? |  | 4 6 6 3 9 6 18 8 10 12 18 9 18 90 25 54 3 4 6 5 |

| Used In (next higher assembly): |  |
| --- | --- |

| Vendor Name | PO/Contract Number |
| --- | --- |

Data Package, Receiving/Inspection Remarks:

| Inspection Required Y/N | Visual Damage Y/N | Comments | Name/ Initials | Date Comp. |
| --- | --- | --- | --- | --- |

Process Flow:

| # | Operation | Start Date | Work Area | Instructions | Name/ Initials | Date Comp. |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Clean |  | LLO | per E960022: clean per E960022: Ultrasonic clean in Liquinox for 10 minutes. Rinse in distilled water at least 3 times, changing the rinse water every time. Ultrasonic clean in methanol for 10 minutes. | T.E. | 1/16/08 |
| 2 | Vacuum Bake |  |  | per E960022: 200°C for 48 hrs | T.E. | 1/21/08 |
| 3 | Control Point |  |  | Review/Approve RGA scan | BO’R | 1/22/08 |
| 4 | Wrap & Tag vacuum clean parts |  |  |  | T.E. | 1/22/08 |
| 5 | Ship and Deliver/File paperwork |  |  | Please send to: LHO c/o SEI File one copy of traveler with the DCC. Note: Ship original traveler with these parts. | BO’R | 1/22/08 |
| END: Go to Traveler or procedure associated with next higher assembly processing |

Special Instructions (Handling/Packaging Constraints, Remarks, etc.) or Notes:

These are parts for the enhanced LIGO SEI build at the Hanford site. The gang-barrel nuts were removed for use on the LLO build. They will be replaced by LLO ones