| Originator | Cognizant Engineer | Ext./Phone# | Project | Account Number |
| --- | --- | --- | --- | --- |
| Corey Gray | Ken Mason | 509-372-8116 | E-LIGO SEI HAM |  |

| Dwg/Part Number | Rev | Part Description / Material | Serial Number | Qty |
| --- | --- | --- | --- | --- |
| Accu-Glass Products 2.75” flange |  | Stainless feedthru- 9 Pin with 2.75 CF Flange (we added one more to this at LLO) | (for LHO installation) | 9 |

| Used In (next higher assembly): | HAM chamber |
| --- | --- |

| Vendor Name | PO/Contract Number |
| --- | --- |

Data Package, Receiving/Inspection Remarks:

| Inspection Required Y/N | Visual Damage Y/N | Comments | Name/ Initials | Date Comp. |
| --- | --- | --- | --- | --- |

Process Flow:

| # | Operation | Start Date | Work Area | Instructions | Name/ Initials | Date Comp. |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Clean | 1/15/08 | LLO | per E960022: clean per E960022: Ultrasonic clean in Liquinox for 10 minutes. Rinse in distilled water at least 3 times, changing the rinse water every time. Ultrasonic clean in methanol for 10 minutes. | T.E. | 1/16/08 |
| 2 | Vacuum Bake | 1/17/08 | LLO | per E960022, 200°C for 48hrs | T.E. | 1/21/08 |
| 3 | Control Point |  | LLO | Review/Approve RGA scan | BO’R | 1/22/08 |
| 4 | Wrap & Tag vacuum clean parts |  | LLO |  | T.E. | 1/22/08 |
| 5 | Ship and Deliver/File paperwork |  | LLO | Please send to: Keep at LLO for pod assembly File one copy of traveler with the DCC. Note: Ship original traveler with these parts. | BO’R | 1/29/08 |
| END: Go to Traveler or procedure associated with next higher assembly processing |

Special Instructions (Handling/Packaging Constraints, Remarks, etc.) or Notes:

Some of these have been used at LLO for the pods here the others are kept at LLO for pod assembly