| Originator | Cognizant Engineer | Ext./Phone# | Project | Account Number |
| --- | --- | --- | --- | --- |
| Stephany Foley | Ken Mason | 617-324-5250 | E-LIGO SEI HAM |  |

| Dwg/Part Number |  | Part Description / Material |  | Qty |
| --- | --- | --- | --- | --- |
| D071251 -00 D071251 -01 D071251 -02 D071251 -03 D071251 -04 |  | gang barrel nut, 17-4 PH stainless steel (3_8-16 w_2 x 3.0) gang barrel nut, 17-4 PH stainless steel (3_8-16 w_4 x 2.5) gang barrel nut, 17-4 PH stainless steel (1_2-13 w_2 x 3.0) gang barrel nut, 17-4 PH stainless steel (1_2-16 w_3 x 2.5) gang barrel nut, 17-4 PH stainless steel (1_2-16 w_4 x 2.5) |  | 6 6 3 9 6 |

| Used In (next higher assembly): |  |
| --- | --- |

| Vendor Name | PO/Contract Number |
| --- | --- |

Data Package, Receiving/Inspection Remarks:

| Inspection Required Y/N | Visual Damage Y/N | Comments | Name/ Initials | Date Comp. |
| --- | --- | --- | --- | --- |

Process Flow:

| # | Operation | Start Date | Work Area | Instructions | Name/ Initials | Date Comp. |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Clean |  | LLO | per E960022: clean per E960022: Ultrasonic clean in Liquinox for 10 minutes. Rinse in distilled water at least 3 times, changing the rinse water every time. Ultrasonic clean in methanol for 10 minutes. | T.E. | 1/5/08 |
| 2 | Vacuum Bake | 1/6/08 | LLO | per E960022: 200°C for 48 hrs | T.E. | 1/9/08 |
| 3 | Control Point |  | LLO | Review/Approve RGA scan | BO’R | 1/908 |
| 4 | Wrap & Tag vacuum clean parts |  | LLO |  | T.E. | 1/9/08 |
| 5 | Ship and Deliver/File paperwork |  |  | Please send to: Keep at LLO c/o SEI, Joe Hanson File one copy of traveler with the DCC. Note: Ship original traveler with these parts. | BO’R | 1/18/08 |
| END: Go to Traveler or procedure associated with next higher assembly processing |

Special Instructions (Handling/Packaging Constraints, Remarks, etc.) or Notes:

Note: these items were removed from the batch of items in traveler E070323-00-X. They will be cleaned at and used at LLO—items indended for LLO were delayed in cleaning at LHO.