| Originator | Cognizant Engineer | Ext./Phone# | Project | Account Number |
| --- | --- | --- | --- | --- |
| Michael Fyffe | R. Wooley | 225 686-3118 | ELIGO |  |

| Dwg/Part Number | Rev | Part Description / Material | Serial Number | Qty |
| --- | --- | --- | --- | --- |
|  | 00 | Viewport |  | 7 |

| Used In (next higher assembly): | eLIGO |
| --- | --- |

| Vendor Name | PO/Contract Number |
| --- | --- |

Data Package, Receiving/Inspection Remarks:

| Inspection Required Y/N | Visual Damage Y/N | Comments | Name/ Initials | Date Comp. |
| --- | --- | --- | --- | --- |
| Y |  | Visually inspect per E990190-01-D |  |  |

Process Flow:

| # | Operation | Start Date | Work Area | Instructions | Name/ Initials | Date Comp. |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Clean |  |  | Per E990190-01-D | T.E. | 2-1-08 |
| 2 | Vacuum Bake |  |  | Per E990190-01-D 200 C for 48 hrs. | T.E. | 2-6-08 |
| 3 | Wrap & Tag vacuum clean parts |  |  | Per E990190-01- Cover the glass surfaces with Lenx 90 lens tissue and wrap the part with UHV quality aluminum foil | T.E. | 2-8-08 |
| 5 | Ship and Deliver/File paperwork |  |  | Please send to: Store all parts in the IO section of the clean LLO optics lab. File one copy of traveler with the DCC. Note: Ship original traveler with these parts. | BO’R | 4-22-08 |
| END: Go to Traveler or procedure associated with next higher assembly processing |  |  |  |  |  |  |

Special Instructions (Handling/Packaging Constraints, Remarks, etc.) or Notes:

RGA Scan was 6 feb 08 approved by BO’R