| Originator | Cognizant Engineer | Ext./Phone# | Project | Account Number |
| --- | --- | --- | --- | --- |
| Brian O’Reilly | Ken Mason | 225-686-3116 | ELIGO SEI HAM |  |

| Dwg/Part Number | Rev | Part Description / Material | Serial Number | Qty |
| --- | --- | --- | --- | --- |
| D080001 D080002 |  | Large Trim Mass Small Trim Mass |  | 3 3 |

| Used In (next higher assembly): | SEI |
| --- | --- |

| Vendor Name | PO/Contract Number |
| --- | --- |

Data Package, Receiving/Inspection Remarks:

| Inspection Required Y/N | Visual Damage Y/N | Comments | Name/ Initials | Date Comp. |
| --- | --- | --- | --- | --- |

Process Flow:

| # | Operation | Start Date | Work Area | Instructions | Name/ Initials | Date Comp. |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Clean |  | LLO | per E960022: clean per E960022: Ultrasonic clean in Liquinox for 10 minutes. Rinse in distilled water at least 3 times, changing the rinse water every time. Ultrasonic clean in methanol for 10 minutes. | T.E. | 2-7-8 |
| 2 | Vacuum Bake |  | LLO | per 960022, class A, 200°C for 48 hrs | T.E. | 2-12-08 |
| 3 | Control Point |  | LLO | Review/Approve RGA scan | BO’R | 2-12-08 |
| 4 | Wrap & Tag vacuum clean parts |  | LLO |  | T.E. | 2-13-08 |
| 5 | Ship and Deliver/File paperwork |  |  | Please send to: One for LHO, One for LLO, One for next HAM-ISI File one copy of traveler with the DCC. Note: Ship original traveler with these parts. | BO’R | 4-21-08 |
| END: Go to Traveler or procedure associated with next higher assembly processing |

Special Instructions (Handling/Packaging Constraints, Remarks, etc.) or Notes: