LIGO Laboratory / LIGO Scientific Collaboration

LIGO- T060095-00-E	LIGO	May 12th 2006

Procedure to expose possible cracks in aluminum welds

Riccardo DeSalvo, Yumei Huang

Distribution of this document:

LIGO Science Collaboration

This is an internal working note

of the LIGO Project.

| California Institute of Technology LIGO Project – MS 18-34 1200 E. California Blvd. Pasadena, CA 91125 Phone (626) 395-2129 Fax (626) 304-9834 E-mail: info@ligo.caltech.edu | Massachusetts Institute of Technology LIGO Project – NW17-161 175 Albany St Cambridge, MA 02139 Phone (617) 253-4824 Fax (617) 253-7014 E-mail: info@ligo.mit.edu |
| --- | --- |
| LIGO Hanford Observatory P.O. Box 1970 Mail Stop S9-02 Richland WA 99352 Phone 509-372-8106 Fax 509-372-8137 | LIGO Livingston Observatory P.O. Box 940 Livingston, LA 70754 Phone 225-686-3100 Fax 225-686-7189 |

http://www.ligo.caltech.edu/

We developed a procedure to study possible cracks in the welds.

As a dry run we sawed a 19 mm diameter aluminum bar with an Al2O3 abrasive blade and made photos of the cut before and after etching with undiluted Protex aluminum Etching solution.

The etch lasted for 30-40 sec, and we observed abundant bubble production.

The photos of the results are below.

Small details are visible, see for example figure 2 bottom or figure 3; we expect that if any crack weld or porosity had been present it would have been either visible or become visible after etching (we can expect that the etching solution would penetrate any crack and porosity and expose it by enlarging it).

The etching applied was ~30 s.  In future we should consider 2 to 4 times longer etching times.

We expect to use this technique to test the weld tests samples produced by Tecnoinox.

Fig: 1 As cut sample, top, and after etching, bottom, x10 lens.

The images are 20 mm across.

Fig: 2 As cut sample, top, and after etching, bottom, x60 lens.

The images are 3.5 mm across.

Fig: 3 As cut sample, top, and after etching, bottom, x200 lens.

The images are 1. mm across.