Statement of Work

# Fabrication of High Quality, Wedged, Windows

C1104441-v1

Note to LIGO users: all red text in this template is font type ‘hidden’ and comprises instructions to complete the SOW.  Easier than deleting them, you can hide all red text before saving.  In Word 2010, click File, Options (on the left side), Display (on the left side), and then unclick “Hidden Text”.

The “TEMPLATE” watermark can be removed by clicking Page Layout, Watermark, and then Remove Watermark.

- Scope (LIGO sub-system)

This SOW is for the manufacture, test, and delivery of high quality 6 inch diameter, anti-reflection coated optical windows with a 0.75 degree wedge. The windows are to be used for viewports on the chamber where a wedged optic is needed and on the Septum Plates inside ultra-high vacuum chambers.

Briefly describe the work.  For example: Fabrication of Vacuum Pod components for Advanced LIGO BSC-ISI Seismometers.

- Document Access

Many supplemental documents and specifications are incorporated into and made a part this Statement of Work.  Click on the document links to access these documents from the LIGO Document Control Center (DCC) or go on line to the LIGO Public DCC at https://dcc.ligo.org/ to access the DCC#.

- Commercial Terms and Applicable LIGO Specifications:

Note: The documents listed below are invoked for this Statement of Work and comprise additional requirements which are integral to this Statement of Work.

Important: C080185 and Q0900001 apply to all SOWs. Add/delete others as appropriate.

Check to be sure the latest revisions are specified below (please notify QAME or Systems if this template needs to be updated).

- LIGO-C080185-v1	LIGO Commercial Items or Services Contract General Provisions

- LIGO-Q0900001-v5 	Advanced LIGO Supplier Quality Requirements

- Quality System:

Referring to the above referenced LIGO Specification Q0900001, Suppliers should include a copy of their current ISO 9001, AS9100, or TS16949 certification in their bid package.  Suppliers lacking current certification should send a copy of their Quality Manual with their bid package.

- Parts/Assemblies to be manufactured, Quantity Required, and Inspection requirements:

Note 1: Refer to Section 8.0 for delivery schedule and location.

Note 2: Refer to Section 6.4 for additional inspection requirements.

List all parts to be made, including the public hyperlink to the latest revision, and the total quantity required.  If you have more than ten parts, create a separate drawing document posted to the DCC as a public document, and link here.

| Drawing # | Part Description | Quantity | AQL Number |
| --- | --- | --- | --- |
| LIGO-D1101005-v1 | aLIGO, high quality, .75 deg wedged, 6" Viewport, Optic | 35 | 0.25 |

Small adjustments to these quantities may be made based on the lot size of the Supplier, in order to make most efficient use of the Supplier’s capabilities. Therefore the quotation should include information about the bidder’s lot or batch size for parts processing.

Note 1: Care should be given to the selection of the AQL number.  Consider the amount of time (which equals cost) required to 100% inspect a given number of parts.  Contact QAME for advice.

Note 2: Additional inspection instructions beyond the AQL number can be given – such as 100% inspection of all threaded holes.

- Manufacturing:

# Requirements:

# Suppliers must refer to the LIGO Specifications referenced in Section 3 for additional, and in some cases, non-industry standard requirements.

# Sub-Contracted Work:

# LIGO expects that at least 2/3 (by dollar value) of the contracted work be performed by the Supplier named on the Purchase Order.  The Supplier shall be responsible for all sub-contracted work.

# Precedence:

The drawings typically represent the finished part as needed for use in service.  Suppliers should always contact a LIGO representative to resolve any discrepancies uncertainties in the documentation or instructions. If there is a conflict between the SOW and the specification, the specification has precedence.

# Special Instructions:

# Windows are to be fabricated in accordance with the following specifications -

| Drawing # | Part Description |
| --- | --- |
| LIGO-E070069-v1 | Specifications for High Quality Window Polish, Advanced LIGO |
| LIGO-E070124-v2 | Septum Window Coating Specification |

# 100% dimensional inspection required of thickness and wedge angle.

# Supply witness samples for each coating run.

# Coating performance measurements can be supplied with witness samples.Add special manufacturing notes

# Exclusions:  Add/delete as appropriate

# None.

- End Item Data Package:  Add/delete lines as necessary

Before delivery of the parts, the Supplier shall provide the following data, as a minimum:

- Any as-built modifications (with approval of the LIGO Contracting Officer) as mark-ups to the drawings

- Material certifications

- Inspection reports for polish surface quality and figure error

- Inspection reports for coating AR performance

- Inspection reports of all dimensional features for the number of parts specified per the AQL number and referenced in the AQL table LIGO-Q1100003-v1 and any other inspection requirements detailed in Section 5 of this SOW

- Certificate of compliance for each part number stating conformance to contract and drawing requirements

- Delivery Requirements:

  - Shipping Containers and Packaging:

The contractor is responsible for providing shipping containers and transportation which protects these parts from damage from the transportation environment (weather, handling, accidents, etc.)  and maintains their cleanliness in their original condition.

Note any special packaging requirements here (i.e., wrap in UHV foil and Ameristat).

  - Shipping Destination(s):

The deliveries are FOB at these destinations, i.e. the Supplier has the responsibility for shipping title and control of goods until they are delivered and the transportation has been completed. The contractor selects the carrier and is responsible for the risk of transportation and for filing claims for loss or damage.

Delete shipping destinations that don’t apply to this SOW.  Be sure to reference the shipping abbreviations (i.e., LLO) in the Delivery Schedule if there is more than one shipping destination.

These items will be shipped to:

California Institute of Technology (CIT)

Attn: Mike Smith

LIGO Project MS 100-36

391 S. Holliston Ave.

Pasadena, CA 91125

  - Delivery Schedule:

Partial and/or early deliveries are acceptable.

| Quantity | Ship Date |
| --- | --- |
| 10 | 18-Aug-2011 |
| 10 | 17-Sep-2011 |
| 10 | 17-Oct-2011 |
| 5 | 16-Nov-2011 |

Insert a list or table detailing the delivery requirements (by P/N, as necessary).  Delivery should be specified in weeks ARO (after receipt of order).  Please also specify the shipping destination (i.e. LLO).

Note any first article requirements.  If applicable, the SOW must state upfront that LIGO wants to assemble the first articles for fit check before the rest of the order is completed.

# Text boxes

# LIGO LABORATORY

California Institute of Technology

1200 E. California Blvd.

Pasadena, CA  91125