## Slide 1
COATING RESEARCH & DEVELOPMENT
@ LMA
G. Cagnoli, A. Cajfinger, V. Dolique, G. Cochez, R. Flaminio, D. Forest,
J. Franc, M. Granata, C. Michel, N. Morgado, L. Pinard, E. Saracco
Laboratoire des Matériaux Avancés (LMA) - Lyon
GWADW – Waikoloa, May 14th 2012
in collaboration with:
  T. Epicier & B. Van de Moortèle Centre Lyonnais de Microscopie (CLYM)
E. Härkönen, M. Ritala & M. Leskelä University of Helsinki

## Slide 2
2
Outline
GWADW – Waikoloa, May 14th 2012
Investigation of Multilayer-Coating Loss
Updates on Atomic Layer Deposition

## Slide 3
3
GWADW – Waikoloa, May 14th 2012
Investigation of Multilayer-Coating Loss
in collaboration with T. Epicier & B. Van de Moortèle, CLYM

## Slide 4
4
Thermal Noise of Coatings
GWADW – Waikoloa, May 14th 2012
the sensitivity gravitational-wave interferometers of 2nd and 3rd generation will be limited by coating thermal noise around 102 Hz
coatings are multilayer stacks realized through Ion Beam Sputtering (IBS)
1st Ti:Ta2O5 layer
SiO2 substrate
✕ N
last SiO2 layer
Ti:Ta2O5 layer
SiO2 layer
SiO2: LOW (L) refractive index
Ti:TaO2O5: HIGH (H) refractive index
Advanced Virgo
Virgo technical note VIR–0128A–12

## Slide 5
5
The Story So Far
GWADW – Waikoloa, May 14th 2012
multilayer coatings show more loss than expected
1st clue [J. Franc @ GWADW10]: « mechanical losses of different multilayer coatings
(…) have been measured and confirm larger losses than expected. »
 thickness of Ti:Ta2O5 is NOT relevant…
new measures [A. Villar @ LVC – Krakow[*] / E. Saracco @ GWADW11]:
[*] LIGO technical note G1000937
 the trend is confirmed
…as the NUMBER OF INTERFACES matters.
characterization [R. Flaminio @ Amaldi 9]:
 linear dependence of loss wrt number of interfaces
credits: E. Saracco
credits: R. Flaminio

## Slide 6
6
Later Developments
GWADW – Waikoloa, May 14th 2012
physico-chemical characterization of SiO2/Ti:Ta2O5 interfaces:
  sample: ITM-HR coating, 1.031H(1.3927L 0.5854H)8 1.199L [18 layers]
hypothesis: interdiffusion of materials?
  imagery
  density profiles
  energy-dispersive X-ray analysis (EDX)  atomic contentration
Focused Ion Beam Microscope
Transmission Electron Microscope
  Scanning/Transmission Electron Microscopy (SEM/TEM) @ CLYM: study at atomic scale

## Slide 7
7
Preparation of the Sample
GWADW – Waikoloa, May 14th 2012
50 nm-thick blade

## Slide 8
8
Tomography & Density Profiles
GWADW – Waikoloa, May 14th 2012
[SEM]
density profiles
depth
[SEM]
measures give expected coating thickness and show no defects
xy
yz
3D tomography
[SEM]
depth
[TEM]
SiO2
Ti:Ta2O5
Ti:Ta2O5
smooth transition between layers
gradient of concentration at interface
   materials do mix

## Slide 9
9
The Picture
GWADW – Waikoloa, May 14th 2012
analyses reveal a mixing interface of 20 to 35 nm
simulated optical spectra of multilayer coatings with mixed materials at
  interfaces are compatible with measures on 1" substrate
line = SIMULATION
circles = DATA
optical simulations also show that gradients should be symmetric:
Ti:Ta2O5 and SiO2 diffuse into each other
analyses of atomic concentrations are not conclusive  new measures in progress
no cristalline phase observed in layers

## Slide 10
10
Mixed Materials
GWADW – Waikoloa, May 14th 2012
[TEM]
50 nm
could mixed interfaces explain exceeding loss?
simple model of the interface: discrete gradient
  mixed material 1 = 65% SiO2 + 35% Ti:Ta2O5
    mixed material 2 = 65% Ti:Ta2O5 + 35% SiO2
mix 2
mix 1
100% Ti:Ta2O5
100% SiO2
to be done: deposit
and measure mix 2
measure of loss of mix1:
Φmix1 = (2.7 +/- 0.2) × 10-4
setup for ringdown technique
loss similar to Ti:Ta2O5
coating of a SiO2 blade with mixed material 1

## Slide 11
11
Interfaces – Results
GWADW – Waikoloa, May 14th 2012
theory:
mix1 = 65% SiO2 + 35% Ti:Ta2O5
mix2 = 65% Ti:Ta2O5 + 35% SiO2
ΦTi:Ta2O5 = (2.4 +/- 0.4) × 10-4
ΦSiO2 = (4.6 +/- 0.1) × 10-5
Φmix1 = (2.7 +/- 0.2) × 10-4
Φmix1 = Φmix2 [assumption]
YTi:Ta2O5 = 140 Gpa
YSiO2 = 73 Gpa
Ymix1 = 65% YSiO2 + 35% YTi:Ta2O5
Ymix2 = 65% YTi:Ta2O5 + 35% YSiO2
Φk : loss angle of the material
tk : total thickness of the material
Yk : Young’s modulus
interfaces only partly fill the gap

## Slide 12
12
Interfaces – Conclusions
GWADW – Waikoloa, May 14th 2012
  excess of mechanical loss is observed in multilayer coatings, depending on the number of interfaces between layers
  interfaces have been characterized
     analyses revealed a mixing zone with gradients of atomic concentration
  … but the presence of mixing interfaces only partially explains the exceeding loss [mixed material 2 has to be measured]
  loss of a mixed material (65% SiO2 + 35% Ti:Ta2O5) has been measured
     loss is similar to that of Ti:Ta2O5 …
do we need a more complex model of the gradient?

## Slide 13
13
GWADW – Waikoloa, May 14th 2012
Updates on Atomic Layer Deposition
in collaboration with E. Härkönen, M. Ritala & M. Leskelä University of Helsinki

## Slide 14
14
GWADW – Waikoloa, May 14th 2012
the idea:
investigation of new techniques to improve quality of coatings
 we want lower mechanical losses
test of ALD realized @ University of Helsinki
Atomic Layer Deposition (ALD)
[*] O Hahtela & al., J. Micromech. Microeng. 17, 2007
       coatings of good quality factors[*] and optical properties
advantages:
self-limiting mechanism of film growth
excellent coating uniformity - even on large areas
homogeneous stoichiometry
high reproducibility
major concern:
low deposition rate

## Slide 15
15
Reminder
GWADW – Waikoloa, May 14th 2012
method based on alternate saturative surface reactions
credits: J. Franc
purge [N2 – 5 s pulse]
precursor 1
[Ta(OCH2CH3)5 – 0.3 s pulse]
purge [N2 – 5 s pulse]
precursor 2 [H2O – 0.3 s pulse]
purge[N2 – 5 s pulse]
 back to step 2
substrate @ T = 250 °C

## Slide 16
previous measurements: J. Franc @ GWADW11 / R. Flaminio @ Amaldi 9
16
ALD – Results
GWADW – Waikoloa, May 14th 2012
monolayer coatings of undoped Ta2O5 on SiO2 cantilever blades
(ΦTa2O5)ALD > (ΦTa2O5)IBS

## Slide 17
17
ALD – Results
GWADW – Waikoloa, May 14th 2012
previous measurements: J. Franc @ GWADW11 / R. Flaminio @ Amaldi 9
monolayer coatings of undoped Ta2O5 on 6 SiO2 substrates of 1"
IBS: n = 2.035
lowest absorption of ALD @ 600 °C: 0.26 ppm – IBS: 1.2 ppm
absorption is highly dependent on annealing temperature
 do the material structure change?

## Slide 18
18
ALD – Conclusions
GWADW – Waikoloa, May 14th 2012
  ALD coatings show good optical absorption
   unusual behavior wrt annealing might be worth further investigation
  ALD is a well-estabilished technique to realize high-quality coatings
  mechanical losses of ALD coatings are larger
   no specific advantage in using ALD instead of IBS
  deposition rate is low

## Slide 19
19
Summary
GWADW – Waikoloa, May 14th 2012
  mixed interfaces can only partly explain the gap between predicted and measured losses
  analyses revealed interfaces of mixed materials
  the structure of multilayer coatings has been characterized
  ALD coating technique has been investigated
    losses are larger compared to IBS coatings
    optical absorption seems lower for Tannealing > 600 °C
  next step: further characterization of optical absorption wrt Tannealing

## Slide 20
20
GWADW – Waikoloa, May 14th 2012
              Thank you for your attention.