| AUTHOR: | CHECKED: | DATE | APPROVALS |
| --- | --- | --- | --- |
|  |  |  | DCN NO. | REV | DATE |
| G. Billingsley | P. Fritschel | 5/29/13 | E1300499 | V1 | 5/29/13 |

| Type | FM |
| --- | --- |
| Purpose | The goal is to demonstrate the existing CSIRO coating uniformity. The coated flat will eventually be used as a metrology reference surface. |
| Applicable Documents |
| Blank Specification | E080045-A – Heraeus Suprasil 312 |
| Polish Specification | E080515-v3 |
| Polish Drawing (Fabricate From) | D080661-v2 |
| General to Surfaces 1 & 2 |
| Figure Change Before / After Coating | Goal: Over a 225 mm diameter aperture, coating uniformity & stress from the coating process shall not change the Sagitta more than 8 nanometers, and shall not add surface figure Zernike terms higher than second order with amplitude > 0.5 nanometers. |
| Coating Deposition Method | Ion Beam Sputtered |
| Coating Area | To Bevel |
| Surface 1 ARROWS ON OPTIC SIDE POINT TO SURFACE 1 |
| Angle of Incidence | 0 degrees |
| Surface 2 |
| Coating Type | Antireflection – optional for stress demonstration |
| Additional Deliverables |
| Layer Thickness Information | For all layers in the design: designed thicknesses, and indices of refraction at 1064 nm for both coating materials (based on individual layers). |