## Slide 1
SUMMARY OF 4” WAFER DATA
Contamination Control Working Group
February 26, 2014

## Slide 2: 4” Wafer & 1” Optic Placement

## Slide 3: Total Wafers Collected
Chart: Number of wafers
| HAM1 | HAM2 | HAM3 | HAM4 | HAM5 | HAM6 | BSC1 | BSC2 | BSC3 | WBSC6* | WBSC9 / LBSC4 | WBSC10 / LBSC5 | Other
Hanford | 0 | 11 | 0 | 0 | 0 | 0 | 1 | 1 | 1 | 2 | 0 | 0 | 1
Livingston | 0 | 18 | 18 | 2 | 0 | 0 | 5 | 6 | 5 | 0 | 0 | 0 | 1

## Slide 4: Total Wafers Collected
Chart: Orientation
| Horizontal | Vertical
Hanford | 16 | 1
Livingston | 45 | 10
  Need more samples for analysis.

## Slide 5: Analysis Progress
Counting microscope setup altered & upgraded.
Must re-scan older wafers.
Good start, there’s more work to do.
Chart: Any Scan Settings
| Scanned | Need to scan
 | 60 | 12
Chart: New Scan Settings
| Scanned | Need to scan
 | 42 | 30

## Slide 6: LBSC1 PCLs
Chart: Particle diameter (µm)
| 3.2866548386940653
65 | 1 | 10000000
100 | 1 | 10000000
150 | 1 | 10000000
300 | 1 | 10000000
500 | 1 | 10000000
750 | 1 | 10000000
65 | 1105.2038 | 389.9749 | 131.0516 | 17.1325 | 1
100 | 5058.2466 | 1784.8195 | 599.7911 | 78.411 | 4.5768 | 1
150 | 24263.6176 | 8561.4999 | 2877.104 | 376.1255 | 21.954 | 4.7968 | 1
300 | 480901.4782 | 169687.7206 | 57023.7944 | 7454.7542 | 435.1247 | 95.0728 | 19.8199 | 1
500 | 5564044.4659 | 1963291.9961 | 659767.0041 | 86251.7287 | 5034.4057 | 1099.9947 | 229.3164 | 11.57 | 1
750 | 45112297.9979 | 15918027.6372 | 5349275.3124 | 699313.9093 | 40818.0797 | 8918.5644 | 1859.2569 | 93.8078 | 8.1078 | 1
log vs log2 graph
502
Floor below ITMY (Vertical)
+Y edge of chamber
344
June – Sept 2013
1 cycle (pump down & vent)
No work
Floor below ITMY (Vertical)
166
200
Floor below ITMY
Sept – Nov 2013
1 cycle
*Work is unknown*
Goal for vertical surfaces
Goal for horizontal surfaces

## Slide 7: LBSC2 PCLs
Mar – June 2013
0 cycles
Heavy work & foot traffic
Chart: Particle diameter (µm)
| 3.2866548386940653
65 | 1 | 10000000
100 | 1 | 10000000
150 | 1 | 10000000
300 | 1 | 10000000
500 | 1 | 10000000
750 | 1 | 10000000
1,000 | 1 | 10000000
1,500 | 1 | 10000000
65 | 1105.2038 | 389.9749 | 131.0516 | 17.1325 | 1
100 | 5058.2466 | 1784.8195 | 599.7911 | 78.411 | 4.5768 | 1
150 | 24263.6176 | 8561.4999 | 2877.104 | 376.1255 | 21.954 | 4.7968 | 1
300 | 480901.4782 | 169687.7206 | 57023.7944 | 7454.7542 | 435.1247 | 95.0728 | 19.8199 | 1
276
Floor below BS
June – Sept 2013
1 cycle
No work
Floor below BS (Vertical)
1,958
Sept – Nov 2013
1 cycle
*Work is unknown*
Floor below BS
Floor below BS (Vertical)
218
233
Chart: Particle diameter (µm)
| 3.2866548386940653
65 | 1 | 10000000
100 | 1 | 10000000
150 | 1 | 10000000
300 | 1 | 10000000
500 | 1 | 10000000
750 | 1 | 10000000
1,000 | 1 | 10000000
1,500 | 1 | 10000000
65 | 1105.2038 | 389.9749 | 131.0516 | 17.1325 | 1
100 | 5058.2466 | 1784.8195 | 599.7911 | 78.411 | 4.5768 | 1
150 | 24263.6176 | 8561.4999 | 2877.104 | 376.1255 | 21.954 | 4.7968 | 1
300 | 480901.4782 | 169687.7206 | 57023.7944 | 7454.7542 | 435.1247 | 95.0728 | 19.8199 | 1
-Y edge of chamber
491
-Y edge of chamber
830
Chart: Particle diameter (µm)
| 3.2866548386940653
65 | 1 | 10000000
100 | 1 | 10000000
150 | 1 | 10000000
300 | 1 | 10000000
500 | 1 | 10000000
750 | 1 | 10000000
1,000 | 1 | 10000000
1,500 | 1 | 10000000
65 | 1105.2038 | 389.9749 | 131.0516 | 17.1325 | 1
100 | 5058.2466 | 1784.8195 | 599.7911 | 78.411 | 4.5768 | 1
150 | 24263.6176 | 8561.4999 | 2877.104 | 376.1255 | 21.954 | 4.7968 | 1
300 | 480901.4782 | 169687.7206 | 57023.7944 | 7454.7542 | 435.1247 | 95.0728 | 19.8199 | 1
-Y edge of chamber
-Y edge of chamber
276
Floor below BS
Floor below BS (Vertical)
1,958
Floor below BS
Floor below BS (Vertical)
218
233
491
830

## Slide 8: LBSC3
Chart: Particle diameter (µm)
| 3.2866548386940653
65 | 1 | 10000000
100 | 1 | 10000000
150 | 1 | 10000000
300 | 1 | 10000000
500 | 1 | 10000000
750 | 1 | 10000000
1,000 | 1 | 10000000
65 | 1105.2038 | 389.9749 | 131.0516 | 17.1325 | 1
100 | 5058.2466 | 1784.8195 | 599.7911 | 78.411 | 4.5768 | 1
150 | 24263.6176 | 8561.4999 | 2877.104 | 376.1255 | 21.954 | 4.7968 | 1
300 | 480901.4782 | 169687.7206 | 57023.7944 | 7454.7542 | 435.1247 | 95.0728 | 19.8199 | 1
500 | 5564044.4659 | 1963291.9961 | 659767.0041 | 86251.7287 | 5034.4057 | 1099.9947 | 229.3164 | 11.57 | 1
Floor below ITMX (Vertical)
+X edge of chamber
402
395
June – Sept 2013
1 cycle
No work
Floor below ITMX (Vertical)
153
337
Floor below ITMX
Sept – Nov 2013
1 cycle
*Work is unknown*

## Slide 9: WBSC Chambers
Chart: Particle diameter (µm)
| 3.2866548386940653
65 | 1 | 10000000
100 | 1 | 10000000
150 | 1 | 10000000
300 | 1 | 10000000
500 | 1 | 10000000
750 | 1 | 10000000
1,000 | 1 | 10000000
1,500 | 1 | 10000000
65 | 1105.2038 | 389.9749 | 131.0516 | 17.1325 | 1
100 | 5058.2466 | 1784.8195 | 599.7911 | 78.411 | 4.5768 | 1
150 | 24263.6176 | 8561.4999 | 2877.104 | 376.1255 | 21.954 | 4.7968 | 1
300 | 480901.4782 | 169687.7206 | 57023.7944 | 7454.7542 | 435.1247 | 95.0728 | 19.8199 | 1
Feb – Oct 2013
1 cycle
Work in adjacent chambers
WBSC1 – Floor below ITMY
230
Oct – Nov 2013
1 cycle
No work?
WBSC3 – Floor below ITMX
316
April – Oct 2013
1 cycle
Heavy work over wafer
WBSC2 – Floor below baffle?
598
  Need more samples to determine trends.

## Slide 10: LHAM2 History
First clean – basic wipe down.
Estimated ~ 1 hour.
Big clean – multiple wipe downs over a 2 week period.
1-1.5 hrs per chamber. Wiped all horizontal & vertical surfaces, top & inside of ISI, underneath support tubes, etc.
Chart: 
| 1 | Pump down #1 (doors close) | Vent (doors open) | 1//2/3/4 | Pump down #2 | Vent | 2 | 3/4/5 | 5 | 6 | Pump down #3 | Vent | 6/7 | Pump down #4 | Vent | 7
POSITION | -50 | 30 | 20 | -50 | 10 | 10 | -50 | -50 | -50 | -50 | 25 | 20 | -50 | 50 | 40 | -50
DATE | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1
Pump down #1
(doors close)
Pump down #2
Vent (doors open)
Vent
Pump down #3
Vent
Pump down #4
Vent
1 cycle
Medium work
(PRM, ISS PD array, PR3 gluing)
1 cycle
Light work
(IO baffles installed)
1 cycle
No work
Med. work
Medium work
(PRM, ISS PD array, PR3 gluing)
1 cycle
Minimal work
1 cycle
Light work
(PR2/PR3 baffles)
First clean – basic wipe down.
Estimated at 1 hour.

## Slide 11: LHAM2
Chart: 
| 1 | Pump down #1 (doors close) | Vent (doors open) | 1//2/3/4 | Pump down #2 | Vent | 2 | 3/4/5 | 5 | 6 | Pump down #3 | Vent | 6/7 | Pump down #4 | Vent | 7
POSITION | -50 | 30 | 20 | -50 | 10 | 10 | -50 | -50 | -50 | -50 | 25 | 20 | -50 | 50 | 40 | -50
DATE | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1
Chart: Particle diameter (µm)
| 3.2866548386940653
65 | 1 | 10000000
100 | 1 | 10000000
150 | 1 | 10000000
300 | 1 | 10000000
500 | 1 | 10000000
750 | 1 | 10000000
1,000 | 1 | 10000000
1,500 | 1 | 10000000
65 | 1105.2038 | 389.9749 | 131.0516 | 17.1325 | 1
100 | 5058.2466 | 1784.8195 | 599.7911 | 78.411 | 4.5768 | 1
150 | 24263.6176 | 8561.4999 | 2877.104 | 376.1255 | 21.954 | 4.7968 | 1
300 | 480901.4782 | 169687.7206 | 57023.7944 | 7454.7542 | 435.1247 | 95.0728 | 19.8199 | 1
+X end of table, on mass
293
+X end of table, on mass
424
In front of MC1 & MC3
322
+X end of table, on mass
*not sealed
188*
Chart: Particle diameter (µm)
| 3.2866548386940653
65 | 1 | 10000000
100 | 1 | 10000000
150 | 1 | 10000000
300 | 1 | 10000000
500 | 1 | 10000000
750 | 1 | 10000000
1,000 | 1 | 10000000
1,500 | 1 | 10000000
65 | 1105.2038 | 389.9749 | 131.0516 | 17.1325 | 1
100 | 5058.2466 | 1784.8195 | 599.7911 | 78.411 | 4.5768 | 1
150 | 24263.6176 | 8561.4999 | 2877.104 | 376.1255 | 21.954 | 4.7968 | 1
300 | 480901.4782 | 169687.7206 | 57023.7944 | 7454.7542 | 435.1247 | 95.0728 | 19.8199 | 1
In front of PR3
In front of PR3
In front of PR3
In front of PR3
218
817
280
268
Chart: Particle diameter (µm)
| 3.2866548386940653
65 | 1 | 10000000
100 | 1 | 10000000
150 | 1 | 10000000
300 | 1 | 10000000
500 | 1 | 10000000
750 | 1 | 10000000
1,000 | 1 | 10000000
1,500 | 1 | 10000000
65 | 1105.2038 | 389.9749 | 131.0516 | 17.1325 | 1
100 | 5058.2466 | 1784.8195 | 599.7911 | 78.411 | 4.5768 | 1
150 | 24263.6176 | 8561.4999 | 2877.104 | 376.1255 | 21.954 | 4.7968 | 1
300 | 480901.4782 | 169687.7206 | 57023.7944 | 7454.7542 | 435.1247 | 95.0728 | 19.8199 | 1
In front of PR3
In front of PR3
In front of PR3
In front of PR3
Near PR3, N door (Vertical)
NW corner of table
N side of table (Vertical)
218
817
280
268
105
218
192

## Slide 12: LHAM2 Story
Chart: 
| 1 | Pump down #1 (doors close) | Vent (doors open) | 1//2/3/4 | Pump down #2 | Vent | 2 | 3/4/5 | 5 | 6 | Pump down #3 | Vent | 6/7 | Pump down #4 | Vent | 7
POSITION | -50 | 30 | 20 | -50 | 10 | 10 | -50 | -50 | -50 | -50 | 25 | 20 | -50 | 50 | 40 | -50
DATE | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1
Pump down #1
(doors closed)
Pump down #2
Vent (doors open)
Vent
Pump down #3
Vent
Pump down #4
Vent
1 cycle
Medium work
280 - 817
1 cycle
Light work
322
1 cycle
No work
293
Med. Work
188*
Medium work
218 - 268
1 cycle
Minimal work
105
1 cycle
Light work
192 - 218

## Slide 13: Summary
Cleaning as you go works!
  Refer to LIGO-G1301249
Upcoming…
  Compiling WHAM data
  1” optic counts & damage plan
  Trips to LHO to continue CC support
  Opportunity for another round of data when ITM’s open in April at LHO

## Slide 14: Relevant Documents
LIGO-F1200021 Advanced LIGO Particulate Sample Form (updated)
LIGO-T1300014 Aligo, BSC Flooring + HAM ISI, Witness Sample Placement Guidelines
LIGO-E1201096 Contamination Sample Handling – How to receive, use, send, buy, and store samples