## Slide 1: Optical Simulation vs Reality at LLO Hiro Yamamoto LIGO lab/Caltech
Introduction
Arm loss
  Loss by COC data and modeling
  Measured loss to total loss
  Effect of LMA coating
Arm modes
  Effective RoC and locations of HOM peaks
Contrast Defect
  400ppm measurement vs 300ppm model
    Various sources of CD, what’s missing?
  ITMY lens and transmission maps, BS maps etc

## Slide 2: aLIGO optics scattering loss by wavelength
2
7.83mm

## Slide 3: COC data and modeling
 | Spatial resolution | coverage | Main use
Phase map | > 1mm | < 2 x 10-4 rad, < 1m at 4km | Field in cavity and near the outer edge of mirror, cavity mode
PSD, RMS | 1μm ~ a few mm by PMM, + phase map | ~ large angle | Characterization of continuous structure, field scattered at large angle
Integrating sphere | fraction of mm | > 5 degree | Total scattering to all angle, effects of non contiguous structures captured. Hole at forward is covered by others.
COC data (characteristics of mirror) +
appr. Maxwell eq. with rigorous boundary cond.
⇒ IFO observable

## Slide 4: Details of ETM09 spiral effect
4
Real PD diameter is ¼ of
Field going to ITM
ETM09 map
Spiral component
8mm
50cm = 1.064μm / (8mm/4000m)

## Slide 5: Noise injection by the spiral pattern on test mass coatings
Phasemap resolution in simulation
Figure loss by two mirrors
~ 15-20ppm
micro roughness, point scattering ~ 20 ppm
7.83mm
ETM07 map
T1300354 by PF,HY
main beam ⇒
ETM reflection ⇒
larger angle scattering into cone ⇒
reflected by beam tube baffles ⇒
back scattered into ETM ⇒
merged into the main beam

## Slide 6: Loss : measurement vs model with COC data
alog13414 ETMY scattering
  Total : 36ppm
  Point scattering : 18ppm
alog13769 Best round trip loss 85ppm
  Extra 30-40ppm, where???
COC data + Model
  Round trip loss error < 14ppm
  Integrated scattering
    7.5ppm by LMA
    9.3ppm by Caltech
  Zygo rms ⇒ loss(<1mm) < 1ppm
  PSD ⇒ loss(<5mm) < 1ppm
Phasemap and Caltech/LMA scattering loss measurements

## Slide 7: Analytic formula in the forward region Huygen’s integral with Fresnel appr.
small aberration
Fresnel approx
Tiny source : dF ⇒ const BRDF ⇒ 2π dS / λ2 x true scattering
PSD to dF :
Δ : 2D amplitude spectral density, ε~1/a few cm

## Slide 8: Baffle PD capturing ETMY scatter phasemap resolution ~ 2mm ⇒ covers 1m
 | PD1 | PD2 | PD3 | PD4
location (mm) | 200 | 438 | 435 | 217
data | 768 | 118 | 48 | 352
FOGP | 863 | 15 | 3 (5) | 625
BRDF on ITMY baffle PD
Real PD diameter is ¼ of
PSD(f)=2500 f(m)-2 nm2 mm
⇒ BRDF = 20 (big error) at 45cm
by using Huygen+Fresnel
Field going to ITM

## Slide 9: Details of ETM09 spiral effect PD1,4 edge of central peak, PD 2,3 edge of 50cm ring
10-5
4.3ppm

## Slide 10: Loss vs ITM tilt alog14171
Log(P) on ITM
Log(P) on ETM
Something is not understood

## Slide 11: LMA coating and arm modes
ETM09 map
Zernike(n+m≤17)
Arm loss = 80ppm
CD = 280
PRG = 40

## Slide 12: Effective RoC and modes

## Slide 13: HOM peak and effective RoC

## Slide 14: Arm scan : alog 14022 To do : calibrate the VCO linearity and refine (and add errors to) the data analysis. VCO sweep was not completely nice and linear.

## Slide 15: Contrast Defect 412ppm : alog13916
-11.6nm
6.6nm
 | No BS aperture | BS02 | BS05
no lens no abr | 44 | 200 | 82
lens abr | 165 | 280 | 300
lens no abr | 120 | 260 | 230
no lens abr | 60 | 200 | 100
CR only CD, no TCS
Beam center mismatch ⇒ (a / 2w)2 = 100ppm for a=1mm

## Slide 16: TCS corrections for LLO PRMI
log11140 CD~400ppm, PRG~45
log#9733 CD~600ppm, PRG~35
RH optimal lens = n(SiO2) x 82km = 1/0.84 x10-5
CP optimal lens = 82km = 1/1.22 x10-5

## Slide 17: (In)Sensitivity on ITM SPTWE + CP lens
ITM08 / ITMY
transmission map in 160mm w/o power
ITM04 / ITMX
-11.6nm
6.6nm
-4.5nm
7.7nm

## Slide 18: Cavity mode
Recycling cavity mode is defined by RM HR reflection and ITM reflection, Ein to Eout, not Ein to Eref, just the same as length case
Optimal coupling is mode(Eref) = mode(Eleak), which makes mode(CR in RC) = mode(SB in RC)
When thermal lens changes, mode(CR in RC) does not change in the first order, but the mode(SB in RC) changes in the first order
But, CR suffers in the second order