## Slide 1: Thermal Noise in Thin Silicon Structures
Matthew Winchester
Mentors: Nicolas Smith, Zach Korth, and Rana Adhikari
August 20, 2015

## Slide 2: Overview
Motivation
Thermal noise
Damped oscillator review
Fluctuation-Dissipation Theorem
Experimental design
Measurements
Conclusions

## Slide 3: Motivation – Increase Future Detector Sensitivity
Reduce thermal noise in suspensions and test masses
Current detectors use fused silica
Crystalline silicon is being considered for future detectors
  Favorable material properties (more on this later)

## Slide 4: Thermal Noise in LIGO
Temperature is a measure of average kinetic energy
Random thermal fluctuations couple to displacement noise in detector
How do we reduce the shaking in our test masses? (without cooling everything to 0K)

## Slide 5: Underdamped Oscillator Review
Equation of motion:
Frequency response:
Underdamped:

## Slide 6: Quality Factor Q

## Slide 7: Internal Damping
Restorative force leads displacement by loss angle ϕ

## Slide 8: How are losses in oscillators related to thermal noise?

## Slide 9: Fluctuation-Dissipation Theorem
FDT relates thermal fluctuations (noise) to dissipation (damping/resistance/loss)
Brownian motion
Johnson noise

## Slide 10: Thermal Noise in Damped Oscillators
Away from resonance:
Thermal noise power spectrum:
We want to design high Q, low loss silicon resonators

## Slide 11: Our Resonators – Silicon Cantilevers

## Slide 12: Silicon Cantilever Design
RIP

## Slide 13: Experimental Design

## Slide 14: Experimental Design

## Slide 15: Experimental Design - Optics

## Slide 16: Experimental Design – Insulation

## Slide 17: Ringdown Measurement
Excite cantilever with impulse and watch free decay

## Slide 18: Continuous Measurement
Cantilever is continuously driven at constant amplitude
Less sensitive to background excitations
Measures Q over temperature sweeps, etc.

## Slide 19: Making Conclusions about Losses
Theory
Simulation
Experiment

## Slide 20: Sources of Loss
Thermoelastic loss
Clamp loss
Surface loss
Phonon-phonon loss
Gas damping
Bulk loss
Excess losses

## Slide 21: Thermoelastic Loss
Coefficient of thermal expansion couples strain to temp.
Heat fluxes driven by temp. gradient dissipate energy

## Slide 22: Thermoelastic Loss cont.
Silicon has a vanishing α at T=125K

## Slide 23: TE Loss Conclusions
Don’t see dramatic increase in Q at 125K
Q is ~2 orders of magnitude lower than TE loss limited prediction
Not TE loss limited

## Slide 24: Clamp Loss
Energy is transferred from cantilever and stored in clamp, base, etc. as strain energy

## Slide 25: Clamp Loss Conclusions
Simulations predict that very little strain energy is stored in clamp, washers, base, etc.
New clamp designs don’t significantly improve Q
Reclamping doesn’t change Q
Not clamp loss limited

## Slide 26: Surface Loss
Surface roughness, lattice imperfections, adsorbed surface materials, etc. contribute to a lossy surface

## Slide 27: Surface Loss Conclusions
Cantilever surfaces clearly show surface defects
Cleaning doesn’t improve Q (?)
Lossy surface layers in simulation accurately predict experimental results
Much more work to be done investigating different etching techniques
Candidate for dominant loss source

## Slide 28: Summary
No quality factor peak at 125K – not TE limited
Simulation shows low strain energy ratios – not clamp loss limited
Most likely surface loss limited – lossy surfaces in simulation match experiment
Developed technique for continuous measurements of several resonant modes simultaneously – speed up future Q measurements

## Slide 29: Future Work
Experiment with different etching techniques
Investigate loss in thin films and optical coatings
Direct thermal noise measurements

## Slide 30: Acknowledgements
My mentors: Zach, Nic, and Rana
Fellow SURF students
LIGO Scientific Collaboration faculty
NSF and Caltech
Thanks for a great summer!

## Slide 31: Questions?

## Slide 32: COMSOL Mode Simulations
Fundamental mode
2nd mode
Normal Modes
3rd mode
Torsional Modes
Fundamental mode
2nd mode