## Slide 1
LIGO-G1602149-v1
APS Division of Laser Science Business Meeting, Rochester, NY, Oct 19, 2016
Seeing Black: Detecting Gravitational Waves From Binary Black Hole Mergers for the First Time Ever using LIGO
David Reitze
LIGO Laboratory
California Institute of Technology
For the LIGO Scientific Collaboration and the Virgo Collaboration

## Slide 2: 2016: Also the Centenary of Gravitational Waves!
Weak field approximation --
space-time is slightly
perturbed from flat space-time:
General Relativity:
Einstein Field Equations
Wave equation for hmn !
Free Space:
Tmn = 0

## Slide 3: Producing Gravitational Waves
h+
Physically, h is a strain: DL/L
hx
worb
R
M
Mass: Stellar Mass Black Holes
Distance: 200 - 600 Mpc
Orbital Frequency: 100-500 Hz
Separation: 3 Schwarzschild radii

## Slide 4: LIGO Interferometry
LIGO uses enhanced Michelson interferometry
  suspended (‘freely falling’) mirrors
Passing GWs stretch and compress the distance between the end test mass and the beamsplitter
The interferometer acts as a transducer, turning GWs into photocurrent
  A coherent detector
Advanced LIGO
4 km

## Slide 5: The astrophysical gravitational wave source catalog
Casey Reed, Penn State
Credit: AEI, CCT, LSU
Coalescing Binary Systems
Neutron stars, black holes
‘chirped’ waveform
Credit: Chandra X-ray Observatory
‘Bursts’
asymmetric core collapse supernovae
cosmic strings
???
NASA/WMAP Science Team
Cosmic GW background
residue of the Big Bang
probes back to 10-21 s
stochastic, incoherent background
Difficult (impossible?) for LIGO to detect
Continuous Sources
Spinning neutron stars
monotone waveform
Notes: LIGO is designed to be an observatory, not a one-off proof that GWs exist. What do we look for?
There are number of predicted astrophysical sources of gravitational radiation, and most of them involve cataclysmic events.
Binary systems – NSs and BHs, most likely source, theoretically well understood with known waveforms
Bursts – GW emissions that are not well modeled or understood. These include asymmetrically core collapse supernova, cosmic strings, and perhaps unknown sources
The residual GW background
Continuously emitting sources such as spinning neutron stars, which have a pure monotone emission.

## Slide 6
The Advanced LIGO Detector

## Slide 7: LIGO
The LIGO Observatories are operated by Caltech and MIT
LIGO Livingston
Observatory
LIGO Hanford Observatory
Hanford, WA
Livingston, LA
LIGO Laboratory:
180 staff located at Caltech, MIT, Hanford, Livingston
LIGO Scientific Collaboration:
~ 1000 scientists, ~80 institutions, 15 countries
Notes: LIGO is actually two observatories and three interferometers.
Describe parameters
Emphasize that the arms are in ultra high vacuum. 8 km of steel 1.2 m dia beam tubes at each site
Separate observatories allow for coincidence detection – since the detectors see uncorrelated noise, only a true gravitational wave would appear on all the interferometers with the correct amplitude.
Emphasize that the LIGO Observatories were designed and are operated by Caltech and MIT

## Slide 8: Advanced LIGO Interferometer
Pre-stabilized Laser
40 kg ‘Test Mass’ Mirror
Quadruple Suspension
Active Seismic Isolation
Input Optics
Output Mode Cleaner
Auxiliary Laser

## Slide 9
2W
35W
180W
Advanced LIGO Pre-Stabilized Laser
Multi-stage Nd:YAG, l=1.06 mm laser
Max Power | 180 W
Power Noise | 10-7 W/Hz-1/2 @ 10 Hz
Frequency Noise | 0.1 Hz/Hz-1/2 @ 10 Hz
165W
P. Kwee, et al., Opt. Exp. 20, 10619 (2012)
Notes: Take out premode cleaner
Take out the NPRO pictures
3 Tera Hz stabilized to 0.1
Get rid of iLIGO stuff

## Slide 10
Advanced LIGO Pre-Stabilized Laser
High Power Mode Quality (200 W)
Laser Frequency Noise
P. Kwee, et al.,
Opt. Exp. 20, 10619 (2012)
Laser Intensity Noise
Notes: Take out premode cleaner
Take out the NPRO pictures
3 Tera Hz stabilized to 0.1
Get rid of iLIGO stuff

## Slide 11: Advanced LIGO ‘Test Mass’ Mirrors
Truly the ‘crown jewels’ of the detector
Physical specifications:
  Ultra-pure, ultra-homogeneous fused silica
  340 mm diameter, 200 mm thick, 40 kg mass
Surface figure: super-polish followed by ion beam ‘spot’ polish
  < 0.15 nm RMS deviation from sphere
Coatings: TiO2-doped Ta2O5/SiO2
  Reflectivity depends upon type of mirror
  Ultralow absorption (< 0.5 ppm)

## Slide 12: The Challenge of Producing LIGO Test Mass Optical Coatings
Figure loss by two mirrors
~ 15-20ppm
micro roughness, point scattering ~ 20 ppm
7.83mm

## Slide 13: Advanced LIGO = Mirror Sensing & Control
Length Sensing and Control: multiple Pound-Drever-Hall length locking
(sensing paths only, actuation paths not shown)
NB: Diagram does not include angular
sensing and control!

## Slide 14: Noises
Fundamental Noises:
Displacement noise
 DL(f)
  Seismic noise
  Radiation Pressure
  Thermal noise
    Suspensions
    Optics
Sensing Noise
 Dtphoton(f)
    Shot Noise
    Residual Gas
Technical Noises:
    Loads of them…

## Slide 15: Nonlinear Effects in Interferometers: Parametric Instabilities
Theory: V. B. Braginsky, S. E. Strigin, and S. P. Vyatchanin, Phys. Lett. A 305, 111 (2002)
Experiment: C. Zhao, L. Ju, J. Degallaix, S. Gras, and D. G. Blair,
Phys. Rev. Lett. 94, 121102 (2005); M. Evans, et al., “Observation of Parametric Instability in Advanced LIGO”, Phys. Rev. Lett. 114, 161102 (2015).

## Slide 16: Observation of Parametric Instabilities in Advanced LIGO
‘Ring Up’ Amplitude vs Time
mechanical mode
Q-factor
power in the
arm cavity
spatial overlap
Optical-mechanical mode
optical mode
gain
Acoustic mode
frequency
Parametric Gain:
Acoustic mode Optical mode
fm = 15,539 Hz
(Parm = 50 kW)

## Slide 17: Tranquilizing Parametric Instabilities
Thermal Tuning of the Mirror
Radii of curvature via Ring Heater
Electrostatic Damping of PI modes

## Slide 18
The First Gravitational Wave Detections

## Slide 19: The First Detection: GW150914
Abbott, et al. ,LIGO Scientific Collaboration and Virgo Collaboration, “Observation of Gravitational Waves from a Binary Black Hole Merger” Phys. Rev. Lett. 116, 061102 (2016)
4 x 10-18 m

## Slide 21: Assessing Statistical Significance: Modeled Search
Matched filter search: X-correlation of L1, H1 data streams with 250,000 BH waveform templates covering 1-- 99 M
Total coincident L1, H1 data: 51.5 days
Background computed from time-shifting coincident data in 100 ms steps to produce 5x106 years
Simulation: Reed Essick, LIGO MIT

## Slide 22: The Sounds of Space-Time

## Slide 23: Parameter Estimation
Abbott, et al. ,LIGO Scientific Collaboration and Virgo Collaboration, “Binary Black Hole Mergers in the first Advanced LIGO Observing Run”, arXiv:1606.04856, Phys. Rev X (to appear)
Hanford
Livingston

## Slide 24: The Black Hole Mass Menagerie
40 Years of X-ray
Astronomy
4 Months of Gravitational-wave Astronomy

## Slide 25
What Comes Next For LIGO?

## Slide 26: Coming Soon: ‘A+’ (A Mid-scale Upgrade of Advanced LIGO)

## Slide 27: Coming Soon: ‘A+’ (A Mid-scale Upgrade of Advanced LIGO)
Quantum (Shot) Noise
Quantum (Radiation
Pressure) Noise
Coating Thermal Noise

## Slide 28: Squeezing: Beating the Quantum Noise Limit
Aasi, et al., (LIGO Scientific Collaboration), Nature Physics, 7, 962 (2011); Nature Photonics 7 613 (2013).
Photodiode
Faraday
Isolator
Squeezed Vacuum
Source
Main Laser
PLL
x1
x2
Squeezed Vacuum
State
3.5 dB squeezing
(1.5X reduced noise)
2.1 dB squeezing
(1.27X reduced noise)
Typical noise without squeezing
Squeezing-enhanced sensitivity
H. P. Yuen, Phys. Rev. A13, 2226 (1976); C. M. Caves, Phys. Rev. D26, 1817 (1982); Wu, Kimble, Hall, Wu, PRL (1986)
Notes: Two demonstrations of squeezing!

## Slide 29: The Problem: Thermal Noise in Optical Coatings
Simple picture: kT of energy per mechanical mode, viscous damping
For coating dominated noise and structural damping:
x()2
 /0
high Q
low Q
x
 1/Q
beam radius
coating thickness
coating elastic loss
signal
band
0
Y. Levin Phys. Rev.
D 57 659 (1998)
Slide Credit:
Marty Fejer, Stanford
Compare: Bulk Silica f ~ 10-6-10-8

## Slide 30: Routes to Improved Coatings with Low Thermal Noise
Goal: 2X – 4X reduction in coating thermal noise
  Path#1: Ultrastable Glasses
  Glasses prepared by physical vapor deposition show extraordinary stability
    slower cooling liquid reaches lower energy states
deposition temperatures, Ts
annealed 350C
X. Liu, F. Hellman, et al, Phys. Rev. Lett. 113, 025503 (2014)
   ~ 2x10-6 vs ~10-4
  Path#2: Crystalline Coatings
  molecular beam epitaxy to generate crystalline GaAs/AlGaAs multilayer
  mirror disc lithography and etch, substrate removal, and direct bonding on substrate
G. D. Cole, W. Zhang, M. J. Martin, J. Ye, and M. Aspelmeyer, Nature Photonics (2013)

## Slide 31: Acknowledgments
Thanks to:
ligo.caltech.edu
www.ligo.org
Support: National Science Foundation
LIGO Livingston Observatory
LIGO Hanford Observatory
LIGO Caltech
LIGO MIT
LSC

## Slide 32
Advanced LIGO and the Dawn of Gravitational-waves Physics and Astronomy
LIGO has made the first measurement of a gravitational wave amplitude and phase
  Merging binary black holes have been observed for the first time
The Advanced LIGO detector is operating at 50% of its design sensitivity
  Will begin running again in late 2016
Upgrades to Advanced LIGO using frequency-dependent squeezing anticipated to begin soon after 2020

## Slide 33: 100th Anniversaries
Inspiration: Eric Gustafson
“Don't do anything that someone else can do. Don't undertake a project unless it is manifestly important and nearly impossible.” Edwin Land
….. Then [gravitational wave amplitudes ] must have a virtually vanishing value in all imaginable cases.” Albert Einstein, 1916

## Slide 34: Some of the Fundamental Questions That Gravitational Waves Can Address
Fundamental Physics
  Is General Relativity the correct theory of gravity?
  How does matter behave under extreme conditions?
  Are black holes truly bald?
Astrophysics, Astronomy, Cosmology
  Do compact binary mergers cause GRBs?
  What is the supernova mechanism in core-collapse of massive stars?
  How many low mass black holes are there in the universe?
  Do intermediate mass black holes exist?
  How bumpy are neutron stars?
  Is there a primordial gravitational-wave residue?
  Can we observe populations of weak gravitational wave sources?
  Can binary inspirals be used as “standard sirens” to measure the local Hubble parameter?
Credit: LIGO Scientific Collaboration
Image credit: W. Benger
Black Hole Merger and Ringdown
Neutron Star Formation
Image credit: NASA
GW Upper limit map

## Slide 35: Phase and Amplitude Squeezing
Amplitude squeezing
Phase
squeezing
Coherent State
ϕ
│E │

## Slide 36: The Best of Both Worlds: Frequency Dependent Squeezing
PLL
Concept: Kimble, Levin, Matsko, Thorne, Vyatchanin, Phys. Rev. D (2001)
Oelker, et al., “Audio-band Frequency-dependent Squeezing”, Phys. Rev. Lett. 116, 041102 (2016).
Notes: Walks through badness, and then sketch path to goodness

## Slide 37: Suppressing Parametric Instabilities
Thermally tuning the test mass radii of curvatures using ring heaters
Active damping via electrostatic feedback through the reaction masses
Passive damping via viscous acoustic mass damping (under development)
unstable region
Had to avoid this mode in the first run

## Slide 38: Low-frequency losses in amorphous dielectrics
Loss mechanism: conventionally associated with low energy excitations (LEEs)
  conceptualized as two-level systems (TLS); Distribution of TLSs arising from disordered structure
  Simple physical mechanism: bond flopping in amorphous materials, e.g. SiO2
E1
E2
V
Δ
Figures: B.S. Lunin
Single TLS
Distribution of TLSs

## Slide 39: Advanced LIGO Suspensions
Force  Displacement
Transfer Function
Model vs. Measured

## Slide 40
https://mediaassets.caltech.edu/gwave