## Slide 1
Multi-Mode Thermal Noise
Experiment, MIT
Slawek Gras, Matthew Evans
a different way of looking
at Coating thermal noise
G1700820

## Slide 2
8
S. Gras, GWADW 2017
13
S. Gras, GWADW 2017
Objectives:
Refine thermal noise estimates for current aLIGO coating,
Test of coating candidates for 3rd generation gravitational wave detectors

## Slide 3
mirror motion, clamping losses, …
(even modes used to avoid alignment sensitivity)
(ties laser frequency to cavity length)
3
S. Gras, GWADW 2017
Multi-mode approach

## Slide 4
large spots on non-sample optics, sample is any 1” HR flat (e.g., typical witness sample)
4
S. Gras, GWADW 2017
Cavity design

## Slide 5
The Experiment
5
S. Gras, GWADW 2017

## Slide 6
S. Gras, GWADW 2017
6
S. Gras, GWADW 2017
The Folded Cavity

## Slide 7
Theory
7
S. Gras, GWADW 2017
Resonant modes

## Slide 8
30 Hz
300Hz
S. Gras, GWADW 2017
Advanced LIGO End Test Mass witness sample:
last year measurement
8
S. Gras, GWADW 2017
S. Gras, H. Yu, W. Yam, D. Martynov, and M. Evans
Phys. Rev. D 95, 022001 (2017)

## Slide 9
30 Hz
9
S. Gras, GWADW 2017
Upgraded readout: sensing noise reduced, better signal-to-noise
3kHz
Advanced LIGO End Test Mass witness sample:
better measurement with upgraded readout

## Slide 10
Slope
measured!
S. Gras, GWADW 2017
10
S. Gras, GWADW 2017
Advanced LIGO End Test Mass witness sample:
higher SNR allows us to measure CTN slope
2 different aLIGO samples measured, similar results

## Slide 11
~ f 0.1
Tantala Loss Angle
3.2
4.0
2.5
11
S. Gras, GWADW 2017
Measured CTN slope consistent with
LMA measurements of tantala loss angle
M. Granata

## Slide 12
12
S. Gras, GWADW 2017
Measurement on LMA coating 'x2-doped' (see Granata’s talk)
Same slope (~ f 0.45) as Advanced LIGO witness sample

## Slide 13
8
S. Gras, GWADW 2017
13
S. Gras, GWADW 2017
Measurement on Lincoln Lab coating
Different slope (~ f 0.47) , CTN ~25% higher than aLIGO witness sample
Coating: λ/4, (1H 1L)18 1H 2L @1064nm
Ta2O5 n=2.10099
SiO2 n=1.47987
T dep. = 120 C, 1.885 A/sec for SiO2
1.934 A/sec for Ta2O5

## Slide 14
8
S. Gras, GWADW 2017
13
S. Gras, GWADW 2017
On-going collaborations and future plans
MIT Lincoln Laboratory:
  coating machine that allows production of new coating designs
  Quick turnaround of coating production
LMA (more details in Granata’s talk)
Coming next:
  study of CTN vs beam spot size
  study of interface losses
  measurement of crystalline coatings

## Slide 15
8
S. Gras, GWADW 2017
14
S. Gras, GWADW 2017
Summary
  So far the MIT multi-mode coating thermal noise experiment has measured two aLIGO samples, one LMA sample, and one test coating from Lincoln Lab
Improved experiment readout allows measurements with high SNR
Recent results
  improved measurement of Advanced LIGO samples shows slope ~ f 0.45
  same slope observed in new LMA coating design (4% higher noise in amplitude over Advanced LIGO sample)
Transitioning to “facility” mode:
  We can measure any 1” flat high reflector
  Mirror swap + measurement now take one day, very quick
  IF YOU HAVE A NEW COATING TO TEST, LET ME KNOW!

## Slide 16: Thanks!

## Slide 17
W. Yam, S. Gras, M. Evans, Budapest 2015
one laser, 2 AOMs: 3 different frequencies
mix of fiber and free space optics
HOM readout is
transmission PDH
CTN readout is HOM
light beat-note
11

## Slide 18: Coating Thermal Noise in TEM02 - TEM20 signal
Intensity
(Intensity Difference)2
Levin Pressure
(for our beam size, coating thickness,
and substrate material)

## Slide 19
Why do we care
about CTN?