## Slide 1: Optical properties of SIlicon for cryogenic Gw detectors
Zeno Tornasi
11/07/2017 - Hilton hotel, Pasadena, ca, U.S.A.
LIGO-G1700998

## Slide 2
Topics
Crystalline silicon
Optical scattering
                Amorphous silicon coatings
                Optical absorption

## Slide 3
Introduction
Why silicon?

## Slide 4
Noise in a gravitational wave detector
Coating Brownian noise
The LIGO Collaboration, Class. Quantum Grav. 32 (2015) 074001

## Slide 5
Temperature
Mechanical loss
Coating thickness
Young’s modulus
Beam width
Coating Brownian noise (similar idea for substrates)
Property of the coating material
Not much to do about it
Limited room for improvement
Substrate engineering constraints
High refractive index materials
Current detectors operate at room T
Can we just go cryogenic then? Not yet…
Property of the material
Can vary by orders of magnitude
Can be engineered to some extent

## Slide 6
Fused silica has a high mechanical loss at low T
Currently LIGO optics are made of fused SiO2
How does the mechanical loss change with T in SiO2?
In general
Travasso F. et al. (2007) Europhys. Lett. 80 50008

## Slide 7
Amorphous silicon looks promising
SiO2
aSi
For coatings, a high refractive index helps (Silicon: 3.47)

## Slide 8
Crystalline silicon looks great too
Low mechanical loss at low temperature.
Christopher Wipf / LIGO-G1700602
Credits: Ronny Nawrodt

## Slide 9
Recap
Both cSi and aSi have low mechanical loss at low temperature
But what about optical properties?
 | cSi (bulk) | cSi (surface) | aSi
Absorption | Bell, A. Markosyan | Ongoing (A. Bell) | This work
Scattering | This work | Future work? | Future work

## Slide 10
Crystalline silicon absorption
Standard Czochralski grown silicon (Cz Si)
    Too impure for application in GW detectors
    because of high optical absorption
Float-zone silicon (FZ Si)
  Very pure and low absorbing: 2 ppm/cm @ 1550 nm
  Available in crystals of maximum diameter 20 cm
Magnetic field-grown Czochralski silicon (MCz Si)
  Available up to 45 cm in diameter
  Bulk absorption can be as low as 5 ppm/cm @ 1550 nm, albeit inhomogeneous
  Occasional surface absorption still under investigation
A. Markosyan, A. Bell / LIGO-G1700480
A. Bell / LIGO-P1700134

## Slide 11
The Glasgow scatterometer
Polariser

## Slide 12
“Engineering run 1”: looking at CCl4
Very lumpy beam despite centrifuging and filtering through 0.2 μm filters
It still looks much better than unfiltered carbon tetrachloride
The peaks sit on a baseline, whose value was used
Obtained scattering ratio 3.5x larger than the value in literature
I had previously performed a rough calibration using the laser itself

## Slide 13
Heraeus Suprasil 3001
fused silica cylinder
(same silica used in LIGO)
Smooth beam
Scattering ratio obtained is 2.16x larger than literature, according to my rough calibration
Or it’s 0.6x literature, taking CCl4 as a reference
TAKE AWAY MESSAGES
Still “commissioning” the scatterometer, plenty of things to understand better
BUT
2. It’s NOT off by orders of magnitude!
“Engineering run 2”: fused silica

## Slide 14
Smooth beam
Difficult to isolate the main beam from the many strong reflections (high refr. index, small polished sample)
Images 10 times brighter than fused silica under similar conditions.
With the current understanding of the instrument, MCz Si scatters
at 1550 nm, at 16° observation angle:
0.11 - 0.17 ppm cm-1 sr-1
0.99 - 1.6 ppm cm-1
“O1”: magnetic Czochralski silicon
Magnetic Czochralski silicon slab

## Slide 15
aSi films were made at UWS
Slides coutesy of prof. Stuart Reid

## Slide 16
Dangling bonds - absorption correlation
Chart: Spins/nm3
| 1.3106178525483844E-2 | 1.3106178525483844E-2 | 1.3106178525483844E-2 | 1.3106178525483844E-2
I16C3110(R)¦0 deg¦JGS1¦579nm | 5181.9548 | 31690.9727 | 19154.2779 | 19249.0501
I16E1708(L)¦200 deg¦JGS1¦242nm | 2450.2841 | 2314.8148 | 1861.0635 | 2727.2727
I16F2008(L)¦400 deg¦JGS1¦459nm | 636.2427 | 824.7744 | 816.1102 | 567.2483
I16H0908 ¦0 deg¦7979¦636nm | 7036.0976 | 6693.6084 | 4546.8204 | 4795.4746
I16H1107(R)¦200 deg¦7979¦523nm | 2227.4183 | 2548.2861 | 2027.4716 | 1955.1685
I16H0408 ¦400 deg¦7979¦548nm | 345.2424 | 327.7767 | 309.5171 | 347.9657
I16C3110(R)¦0 deg¦JGS1¦579nm | 898.1002 | 6849.2269 | 680.5181 | 1043.3642
I16E1708(L)¦200 deg¦JGS1¦242nm | 455.8398 | 390.4395 | 371.2299 | 481.4251
I16F2008(L)¦400 deg¦JGS1¦459nm | 496.4291 | 441.2977 | 448.908 | 503.8549
I16F2008(L)¦400 deg¦JGS1¦459nm | 496.4291 | 441.2977 | 448.908 | 503.8549
I16H0908 ¦0 deg¦7979¦636nm | 145.8385 | 131.9785 | 119.409 | 125.6444
I16H1107(R)¦200 deg¦7979¦523nm | 211.038 | 214.7153 | 227.1079 | 216.1971

## Slide 17
Deposition temperature - absorption correlation
Chart: Deposition temperature [°C]
| 0 | 0 | 0 | 0
I16C3110(R)¦0 deg¦JGS1¦579nm | 898.1002 | 6849.2269 | 680.5181 | 1043.3642
I16E1708(L)¦200 deg¦JGS1¦242nm | 455.8398 | 390.4395 | 371.2299 | 481.4251
I16F2008(L)¦400 deg¦JGS1¦459nm | 496.4291 | 441.2977 | 448.908 | 503.8549
I16H0908 ¦0 deg¦7979¦636nm | 145.8385 | 131.9785 | 119.409 | 125.6444
I16H1107(R)¦200 deg¦7979¦523nm | 211.038 | 214.7153 | 227.1079 | 216.1971
I16H0408 ¦400 deg¦7979¦548nm | 283.777 | 258.9255 | 256.9259 | 285.8381
I16C3110(R) | 5181.9548 | 31690.9727 | 19154.2779 | 19249.0501
I16E1708(L) | 2450.2841 | 2314.8148 | 1861.0635 | 2727.2727
I16F2008(L) | 636.2427 | 824.7744 | 816.1102 | 567.2483
I16H1107(R) | 7036.0976 | 6693.6084 | 4546.8204 | 4795.4746
I16H1107(R) | 2227.4183 | 2548.2861 | 2027.4716 | 1955.1685
I16H0408 | 345.2424 | 327.7767 | 309.5171 | 347.9657

## Slide 18
Conclusions
Silicon is a promising material for cryogenic GW core optics.
It has low mechanical loss at low temperature, zeros of expansion coefficient, high refractive index
In Glasgow a scatterometer is active
It is able to take measurements to better than order of magnitude level but we’re working hard towards a fully reliable instrument
Preliminary measurement of MCz Si suggest values compatible with use in ET.
45-74 ppm bulk scatter for a 46 cm thick test mass would likely be dominated by coating scattering
Heat deposited aSi coatings show absorption comparable with annealed ones.
A clear link has been established between absorption and dangling bonds, and absorption and deposition temperature.

## Slide 19
Future
Optimise the scatterometer, understand its noise sources and discrepancies with literature
Carry out systematic angle-dependent measurements to verify to which extent the scattering observed is really only Rayleigh
Find a way to reliably calibrate the system
Work towards understanding surface absorption (not discussed here)
Integrate the aSi coatings study with other analyses such as Raman spectroscopy

## Slide 20
Thank you!

## Slide 21
Photothermal common-path interferometry (PCI)