## Slide 1: Absorption Test ITM03/11 Witness sample SN1549 LMA Run Reference C13074/13
Microscopy/absorption test/Microscopy
Billingsley/Zhang
December 2019

## Slide 2: HR ITM03/11 Absorber is located in the large circle. Non-absorber in the small circle Image S1, Arrow down. SN1549 LMA ref C13074/13 We believe the /13 refers to the position in the coating chamber. Text is on the container

## Slide 3: Image arrow at -Y

## Slide 4: Close up of absorber circle/position

## Slide 5: Absorber ~13 µm long

## Slide 6: Many other things not absorbing Following are images of things in the scan area that did not register as absorbing.

## Slide 7: Location of the “bubble” non-absorber inside the smaller circle

## Slide 8: Non absorbing roughly 25 µm long no change in appearance before/after Abs. scan

## Slide 9: Non Absorbing. Roughly 10µm long

## Slide 10: See G2000212 for micromachining tests.
Absorber Before
Absorber after 

## Slide 11: Keyence images post ablation on the next slides For comparison – do we need a Leica confocal microscope to determine success?

## Slide 13: Also found near the arrow

## Slide 14: Large spot found in the zone where the absorber was.

## Slide 15: 21.67 µm green dots, 22.16µm horizontal on Keyence

## Slide 16: No surrounding scatter appears in dark field view