## Slide 1: Birefringence Variation in 10 cm Diameter AlGaAs on Silica Mirror
Andri Gretarsson, Breck Meagher Embry-Riddle

## Slide 2: Single-reflection Measurement
Sample angle
(Angle between fast axis and analyzing polarizer)
Fast axis angle wrt. analyzer
Reflected phase shift b/w fast & slow axes
=
Powers in the two polarizations
(beam steering)

## Slide 3: Recent Photo

## Slide 4: Stress-induced birefringence
,

## Slide 5
Before
After
(Non) Effect of Cleaning with First Contact

## Slide 6: Average of Two Scans
Probably
dust
Horizontal lines pattern is due to filtering, but swirly features are real
Al(0.92)Ga(0.08)As/GaAs, TO-optimized stack

## Slide 7: Birefringence Scans
Stress-induced
Birefringence from
Heating
Spatial filter “ringing” due to sudden large stress-induced birefringence nearby (i.e. not real)
Point defects and/or dust
Perpendicular hash pattern is due to filtering, but diagonal features are real
Horizontal lines pattern is due to filtering, but swirly features are real
TiO2(40%)Ta2O5(60%) / SiO2 lambda/4 stack
Al(0.92)Ga(0.08)As/GaAs, TO-optimized stack

## Slide 8: Fast axis of variation is approximately aligned with main birefringence axis