| APPROVALS | DATE | REV | DCN NO. | BY | CHECK | DCC | DATE |
| --- | --- | --- | --- | --- | --- | --- | --- |
| AUTHOR: G. Billingsley | 3-25-26 | V1 | E2600099 |  |  |  |  |
| CHECKED: L. Zhang |  |  |  |  |  |  |  |
| APPROVED: |  |  |  |  |  |  |  |
| DCC RELEASE |  |  |  |  |  |  |  |

# Description

1” Ø Flat/Flat high reflector coated on one side for 0 ° use @ 1064nm

# Material

Corning 7980 Mirror Grade fused silica or equivalent

Grade 0F or better (Low inclusion class: <0.3 mm² cross section, 0.1 mm max. size,

Homogeneity < 5ppm)

# Mechanical Properties Per LIGO-D1301036

1"Ø ± 0.01 x 0.25" ± .01" Plano / Plano

CA = central 80%

Bevels on S1 and S2

# Markings

Each optic should have a unique serial number

An arrow on the barrel points to the HR surface.

The arrow and serial number shall be scribed or etched on the barrel

of the optic for in-vacuum use. No pencil marks shall be present on the optic.

# Surface Roughness

Side 1

Surface Roughness: ≤ 5Å RMS in CA

Surface Quality: 10-5

Side 2

Surface Roughness: < 10Å RMS in CA

Surface Quality: 40-20

Optic Barrel and Bevels

Polished, with no grey evident when inspected in normal room lighting.

# Surface Figure

Side 1

Flat < λ/4 at 632.8 in CA

Side 2

Flat < λ/4 at 632.8 in CA

# Coating

Wavelength: 1064nm

Angle of incidence: 0°5°

Side 1

R >= 99% @ 1064nm

Absorption @ 1064 nm ≤ 1ppm

Side 2

No coating